Product Technical Specification

Product Introduction

CN-102 is a self-matting waterborne polyurethane resin. It contains no matting powder, delivers excellent matting effect, high black transparency, superior resistance to white gasoline, and outstanding high-temperature resistance up to 230℃. The coating surface is non-tacky with good adhesion. It is suitable for surface finishing of leather, paper, films and other substrates. The product meets environmental protection standards of Europe, America and Japan.

Product Features

- Eco-friendly emulsion, free of toxic substances including formaldehyde, nonylphenol, heavy metals, polycyclic aromatic hydrocarbons (PAHs) and DMF.

- Soft and non-tacky surface with excellent flexibility.

- Excellent high-temperature resistance up to 230℃.

- Can be used with our waterborne curing agents (CN-G118/120) to enhance resin performance.

Product Technical Parameters*

| Item | Parameter | Unit | Test Method |
| --- | --- | --- | --- |
| Appearance | Milky white liquid | / | GB/T 14074.1-1993 |
| Solid Content | 30.00±1.00 | % | GB/T 2793-1995 |
| Viscosity | 1000–2000 | mPa·s | GB/T 10247-1998 |
| pH | 6.5–7.5 | / | GB/T 14518-1993 |
| 100% Modulus | 5.0–6.0 | MPa | / |
| Tensile Strength | 17.0–19.0 | MPa | / |

*The above parameters are typical results only and shall not be regarded as specifications. Please refer to the actual COA for details.

Storage

- Store in the original sealed container.

- Recommended storage temperature: 6–32℃.

- Use within 6 months from the production date.

- Avoid direct sunlight and contamination by foreign substances.

Prolonged storage at low temperature may cause irreversible damage to the product. Keep the container tightly sealed; otherwise, water evaporation will form an insoluble polymer film on the surface. Expiry of the 6-month shelf life does not necessarily mean the product is out of specification. Please test before application to verify its compliance.

Precautions

- Slight delamination may occur after long-term storage; stir well before use.

- Waterborne isocyanate, aziridine or carbodiimide crosslinkers can be added to further improve physical and chemical properties.

- As an anionic resin, it is incompatible with other cationic resins or additives. Our polyurethane thickeners are recommended.

- This product contains no preservatives.

The above information is based on our laboratory quality evaluation and is not a guarantee of specific performance or suitability for intended applications. Please conduct necessary tests before use. Thank you for your choice and support!