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Product Technical Specification
Product Introduction
CN-102 is a self-matting waterborne polyurethane resin. It contains no matting powder, delivers excellent matting effect, high black transparency, superior resistance to white gasoline, and outstanding high-temperature resistance up to 230℃. The coating surface is non-tacky with good adhesion. It is suitable for surface finishing of leather, paper, films and other substrates. The product meets environmental protection standards of Europe, America and Japan.

Product Features
1. Eco-friendly emulsion, free of toxic substances including formaldehyde, nonylphenol, heavy metals, polycyclic aromatic hydrocarbons (PAHs) and DMF.
2. Soft and non-tacky surface with excellent flexibility.
3. Excellent high-temperature resistance up to 230℃.
4. Can be used with our waterborne curing agents (CN-G118/120) to enhance resin performance.

Product Technical Parameters*

	Item
	Parameter
	Unit
	Test Method

	Appearance
	Milky white liquid
	/
	GB/T 14074.1-1993

	Solid Content
	30.00±1.00
	%
	GB/T 2793-1995

	Viscosity
	1000–2000
	mPa·s
	GB/T 10247-1998

	pH
	6.5–7.5
	/
	GB/T 14518-1993

	100% Modulus
	5.0–6.0
	MPa
	/

	Tensile Strength
	17.0–19.0
	MPa
	/


*The above parameters are typical results only and shall not be regarded as specifications. Please refer to the actual COA for details.
Storage
1. Store in the original sealed container.
2. Recommended storage temperature: 6–32℃.
3. Use within 6 months from the production date.
4. Avoid direct sunlight and contamination by foreign substances.

	Prolonged storage at low temperature may cause irreversible damage to the product. Keep the container tightly sealed; otherwise, water evaporation will form an insoluble polymer film on the surface. Expiry of the 6-month shelf life does not necessarily mean the product is out of specification. Please test before application to verify its compliance.



Precautions
1. Slight delamination may occur after long-term storage; stir well before use.
2. Waterborne isocyanate, aziridine or carbodiimide crosslinkers can be added to further improve physical and chemical properties.
3. As an anionic resin, it is incompatible with other cationic resins or additives. Our polyurethane thickeners are recommended.
4. This product contains no preservatives.
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	The above information is based on our laboratory quality evaluation and is not a guarantee of specific performance or suitability for intended applications. Please conduct necessary tests before use. Thank you for your choice and support!
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Hefei Conada New Materials Co. , Ltd.




