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Waterborne Polyurethane Dispersion


Product Technical Specification
Product Introduction
CN-301Y is a cationic waterborne polyurethane resin. It is safe, non-toxic, odorless and non-irritating. The film is transparent, smooth, medium-hard, non-sticky with good adhesion. It can be used as a waterborne adhesive or coating for metal, plastics (PVC, PET, PC, ABS, etc.), rubber (NBR, etc.), leather and other substrates. The environmental test results of this product meet the standards of Europe, America and Japan.
Product Features
1. Eco-friendly emulsion, free of toxic substances such as formaldehyde, nonylphenol, heavy metals, polycyclic aromatic hydrocarbons (PAHs) and DMF.
2. Transparent and smooth film, medium-hard and non-sticky surface with excellent flexibility.
3. Excellent adhesion to most substrates.
4. Can be used with our company’s waterborne curing agents (CN-G118/120) to enhance resin performance.
Technical Parameters*

	Item
	Parameter
	Unit
	Test Method

	Appearance
	Bluish translucent liquid
	/
	GB/T 14074.1-1993

	Solid Content
	35.00±1.00
	%
	GB/T 2793-1995

	Viscosity
	＜100.0
	mPa·s
	GB/T 10247-1998

	pH
	4.0–6.0
	/
	GB/T 14518-1993

	100% Modulus
	5.0–6.0
	MPa
	/

	Tensile Strength
	17.0–19.0
	MPa
	/


[bookmark: _GoBack]*These parameters represent typical results only and shall not be deemed as specifications. Subject to the actual Certificate of Analysis (COA).
Storage
1. Store in the original sealed container.
2. Recommended storage temperature: 6–28 °C.
3. Use within 6 months from the production date.
4. Avoid direct sunlight and contamination by other substances.

	Prolonged storage at low temperature may cause irreversible damage to the product. Keep the container tightly sealed; otherwise, water evaporation will form an insoluble polymer film on the product surface. Expiry of the 6‑month shelf life does not necessarily mean the product is out of specification. Please test before application to verify its compliance.



Precautions
1. Adding a curing agent can improve fastness but may affect hand feel.
2. Waterborne resin with crosslinking agent must be used within 24 hours.
3. This product is a cationic resin and shall not be mixed with other anionic resins or additives. Polyurethane thickeners of our company are recommended.







	The above information reflects our internal quality evaluation results from laboratory testing. It is not a guarantee of product performance or suitability for specific applications. Please conduct necessary tests before application. Thank you for your choice and support!
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Hefei Conada New Materials Co. , Ltd.




