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Product Technical Specification
Product Introduction
CN-8201 is an anionic aliphatic waterborne polyurethane dispersion. It forms transparent films with high strength, alcohol-wipe resistance, scratch resistance and friction resistance. The emulsion has high ethanol tolerance and can be used as waterborne coatings and adhesives for metals, plastics, printing inks, etc.
Product Features
1. Excellent water resistance, temperature resistance and yellowing resistance.
2. Waterborne dispersion, free of organic solvents, green and eco-friendly.
3. Outstanding solvent resistance of the coating, especially excellent alcohol-wipe resistance.
4. Dry and non-tacky film surface, tough and strong film.

Product Technical Parameters*
	Item
	Parameter
	Unit
	Test Method

	Appearance
	Clear liquid with blue tint
	—
	GB/T 14074.1-1993

	Solid Content
	30.00±1.00
	%
	GB/T 2793-1995

	Viscosity
	＜500
	mPa·s
	GB/T 10247-1998

	pH
	6.0–9.0
	—
	GB/T 14518-1993

	Density
	1.02–1.09
	g/cm³
	GB/T 4472-2011


*The above parameters represent typical results only and shall not be regarded as specifications. Refer to the actual COA for details.

Storage
1. Store in the original sealed container.
2. Recommended storage temperature: 6–28 °C.
3. Avoid direct sunlight and contamination by other substances.

	Prolonged storage at low temperatures may cause irreversible damage to the product. Keep the container sealed; otherwise, water evaporation will form an insoluble polymer film on the surface.



Storage Period
1. Use within 6 months from the production date.

	Expiration of the 6-month shelf life does not mean the product is out of specification. Test before use to verify compliance with specifications and technical parameters.




Precautions
1. Adding a curing agent can improve fastness but may affect hand feel.
2. Waterborne resin added with crosslinking agent must be used within 24 hours.
3. This product is synthesized with special polyester. The dry film offers excellent water resistance. However, the aqueous emulsion may decompose during long-term storage. Please test in advance before using long-stored product.



	The above information only represents our laboratory quality evaluation results and does not guarantee the product’s performance or suitability for specific applications. Please conduct necessary tests before use. Thank you for your choice and support!
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Hefei Conada New Materials Co. , Ltd.




