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Product Technical Specification
Product Introduction
CN-817-1 is a specially modified anionic waterborne polyurethane resin. It is a peelable, high-gloss, yellowing-resistant waterborne polyurethane emulsion. It features moderate film softness, high strength and fullness, and is a high-performance emulsion specially designed for peelable substrates, especially for ABS/PC and other substrates.

Product Features
1. Small and uniformly distributed emulsion particle size, providing peelability and excellent water resistance to substrates.
2. Milky white with obvious blue light, good leveling and rheological properties, high gloss.
3. Full film formation, moderate softness, and high tensile strength.
4. Good peelability on ABS/PC and other surfaces, superior to similar products on the market.

Product Technical Parameters*
	Item
	Parameter
	Unit
	Test Method

	Appearance
	Milky white with blue light
	—
	GB/T 14074.1-1993

	Solid Content
	42.00±1.00
	%
	GB/T 2793-1995

	Viscosity
	50–5000
	mPa·s
	GB/T 10247-1998

	pH
	6.0–8.0
	—
	GB/T 14518-1993

	Elongation at Break
	400–500
	%
	—

	Tensile Strength
	＞25
	MPa
	—

	100% Modulus
	4.5–5.4
	MPa
	—


*The above parameters represent typical results only and shall not be regarded as specifications. Refer to the actual COA for details.
Storage
1. Store in the original sealed container.
2. Recommended storage temperature: 6–28 °C.
3. Use within 6 months from the production date.
4. Avoid direct sunlight and contamination by acids, alkalis or other substances.

	Prolonged storage at low temperatures may cause irreversible damage to the product. Keep the container sealed; otherwise, water evaporation will form an insoluble polymer film on the surface. Expiration of the 6-month shelf life does not mean the product is out of specification. Test before use to verify compliance with specifications and technical parameters.



Precautions
1. Adding a curing agent can improve fastness but may affect hand feel.
2. Waterborne resin added with crosslinking agent must be used within 24 hours.
3. Do not mix with other cationic resins.








	The above information only represents our laboratory quality evaluation results and does not guarantee the product’s performance or suitability for specific applications. Please conduct necessary tests before use. Thank you for your choice and support!
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