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Product Technical Specification
Product Introduction
HEUR-540B is a liquid waterborne polyurethane thickener. It is easy to use and outperforms traditional cellulose‑based thickeners (such as HEC hydroxyethyl cellulose, MC methyl cellulose, etc.) and acrylic thickeners in leveling, film gloss and water resistance.
Product Technical Parameters*
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	Specification

	Appearance
	Colorless or pale yellow transparent liquid

	Solid content
	40%±1%

	Colloid charge
	Non-ionic

	Viscosity
	3500-8000 mPa·s (25℃)

	Specific gravity
	1.02-1.06 g/cm³


*The above parameters represent typical results only and shall not be regarded as specifications. Refer to the actual COA for details.
Applications
Water-based coatings, water-based adhesives, water-based inks, textile coatings, leather finishing, etc.
Product Features
1. Medium shear thickener.
2. Excellent thickening efficiency, flow and leveling properties.
3. Free of organotin, APEO and other toxic substances.
4. Good dispersibility, assisting wetting and dispersion of pigments.
5. Non-ionic, performance not affected by system pH.
6. No negative impact on product gloss.
Dosage and Application
1. Dosage based on total formulation: 0.2-2.0%. Determine the optimal dosage according to system composition and required fluidity.
2. Can be added before or after grinding. It is recommended to add partly before grinding and partly after grinding.
3. No pre-dilution required. If dilution is needed, use water-based solvents.
Precautions
1. Associative thickening is affected by temperature: higher viscosity at low temperature and lower viscosity at high temperature. Please consider temperature conditions in formulation design.
2. Re-test is required when raw material batches are changed to confirm the proper dosage.
3. Crystallization may occur at low temperature, which does not affect product performance. Heat to melt crystals before use if crystallization occurs.
Storage and Shelf Life
1. Store in original sealed container.
2. Recommended storage temperature: 6-28℃.
3. Use within 12 months from production date.
4. Avoid direct sunlight and contamination.
Packaging
50 kg, 125 kg and IBC tote packages are available. Customizable according to customer requirements.









	The above information only represents our laboratory quality evaluation results and does not guarantee the product’s performance or suitability for specific applications. Please conduct necessary tests before use. Thank you for your choice and support!
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