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Product Technical Specification
Product Introduction
CN-901 is an anionic waterborne polyurethane resin. It is a waterborne polyurethane emulsion with high wear resistance, wash resistance, high gloss and good adhesion. It features moderate film softness, high strength and good toughness, and is a high-performance emulsion specially designed for difficult-to-adhere substrates.

Product Features
1. Small and uniformly distributed emulsion particle size, strong adsorption to fabrics, high crosslink density, and excellent water resistance.
2. Good leveling and rheological properties, high transparency, high gloss, excellent abrasion resistance and soaping fastness.
3. Full film formation with moderate softness; good elasticity and softness maintained even at low temperatures.
4. Good cold resistance.
5. Excellent adhesion to PE/HDPE filament bonding, superior to similar products on the market.

Product Technical Parameters*
	Item
	Parameter
	Unit
	Test Method

	Appearance
	Clear watery liquid
	—
	GB/T 14074.1-1993

	Solid Content
	30.00±1.00
	%
	GB/T 2793-1995

	Viscosity
	>10.0
	mPa·s
	GB/T 10247-1998

	pH
	6.0–9.0
	—
	GB/T 14518-1993

	Elongation at Break
	750
	%
	—

	Tensile Strength
	40.0–45.0
	MPa
	—


*The above parameters represent typical results only and shall not be regarded as specifications. Refer to the actual COA for details.

Storage
1. Store in the original sealed container.
2. Recommended storage temperature: 6–28 °C.
3. Use within 6 months from the production date.
4. Avoid direct sunlight and contamination by other substances.

	Prolonged storage at low temperatures may cause irreversible damage to the product. Keep the container sealed; otherwise, water evaporation will form an insoluble polymer film on the surface. Expiration of the 6-month shelf life does not mean the product is out of specification. Test before use to verify compliance with specifications and technical parameters.




Precautions
1. Adding a curing agent can improve fastness but may affect hand feel.
2. Waterborne resin added with crosslinking agent must be used within 24 hours.
3. Do not mix with other cationic resins.





	The above information only represents our laboratory quality evaluation results and does not guarantee the product’s performance or suitability for specific applications. Please conduct necessary tests before use. Thank you for your choice and support!
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Hefei Conada New Materials Co. , Ltd.




