Product Technical Specification

Product Introduction

CN-206 is an anionic waterborne polyurethane resin. It forms a transparent, moderately hard and tough film with smooth surface and high gloss. This product can be used as a coating for flexible substrates such as garment fabric coating, printing varnish and leather finishing, as well as a binder for water-based inks with good hot-press lamination fastness.

Product Features

- Free of toxic substances such as formaldehyde, nonylphenol, heavy metals, polycyclic aromatic hydrocarbons (PAHs) and DMF.

- Forms a transparent film with good gloss and excellent toughness.

- Excellent elongation and flex resistance.

- Outstanding water resistance, weather resistance and yellowing resistance of the coating.

- Excellent adhesion to most substrates.

Technical Parameters*

| Item | Parameter | Unit | Test Method |
| --- | --- | --- | --- |
| Appearance | Clear with bluish tint | / | GB/T 14074.1-1993 |
| Solid Content | 40.00±2.00 | % | GB/T 2793-1995 |
| Viscosity | >10.0 | mPa·s | GB/T 10247-1998 |
| pH | 6.0–8.0 | / | GB/T 14518-1993 |
| 100% Modulus | 4.89 | MPa | / |
| Tensile Strength | 23–25 | MPa | / |

*These parameters represent typical results only and shall not be deemed as specifications. Subject to the actual Certificate of Analysis (COA).

Storage

- Store in the original sealed container.

- Recommended storage temperature: 6–28 °C.

- Use within 6 months from the production date.

- Avoid direct sunlight and contamination by other substances.

Prolonged storage at low temperature may cause irreversible damage to the product. Keep the container tightly sealed; otherwise, water evaporation will form an insoluble polymer film on the product surface. Expiry of the 6-month shelf life does not necessarily mean the product is out of specification. Please test before application to verify its compliance.

Precautions

- Adding a curing agent can improve fastness but may affect hand feel.

- Waterborne resin with crosslinking agent must be used within 24 hours.

- This product is synthesized with special polyester; the dry film provides excellent water resistance. The waterborne emulsion may degrade during long-term storage, so pre-testing is recommended before use.

The above information reflects our internal quality evaluation results from laboratory testing. It is not a guarantee of product performance or suitability for specific applications. Please conduct necessary tests before application. Thank you for your choice and support!