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Waterborne Polyurethane Dispersion


Product Technical Specification
Main Ingredients
[bookmark: _GoBack]Waterborne aromatic polyurethane resin
Product Features
Waterborne polyurethane dispersion, excellent cost performance, good powder dispersibility, soft hand feel, good foaming property.
Product Technical Parameters*
	Item
	Parameter
	Unit
	Test Method

	Appearance
	Milky white with obvious blue light
	/
	GB/T 14074.1-1993

	Solid Content
	40±2
	%
	GB/T 2793-1995

	pH
	6.0-8.0
	/
	GB/T 14518-1993

	100% Modulus
	0.5~2
	MPa
	/

	Breaking Strength
	≥5
	MPa
	/

	Elongation
	≥500
	%
	/


*The above parameters represent typical results only and shall not be regarded as specifications. Please refer to the actual COA (Certificate of Analysis).
Precautions
Non-hazardous chemical. Sealed storage at 5 ℃~35 ℃, avoid light. Seal tightly after use. Do not mix with cationic pastes or solvent-based pastes.


	The above information only represents our quality evaluation results obtained in our laboratory, and does not guarantee that the product has certain properties or meets specific applications. Please conduct specific tests as required before use. Thank you for your choice and support!
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Hefei Conada New Materials Co. , Ltd.




