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Waterborne Polyurethane Dispersion


Product Technical Specification
Main Components
Waterborne aliphatic polyurethane resin
Product Features
1. Low modulus, high solid content resin for synthetic leather foaming.
2. Suitable for dry-process base of waterborne garment leather; soft hand feel and high fullness.
[bookmark: _GoBack]Product Technical Parameters

	Item
	Parameter
	Unit

	Appearance
	Milky white with obvious blue light
	—

	Solid Content
	47±2
	%

	pH
	6.0~8.0
	—

	100% Modulus
	0.5~1.5
	MPa

	Breaking Strength
	≥5
	MPa

	Elongation
	≥800
	%



Precautions
Non-hazardous chemical. Store sealed at 5 ℃~35 ℃, avoid light. Reseal after use. Do not mix with cationic pastes or solvent-based pastes.

	The above information only represents our laboratory quality evaluation results and does not guarantee the product’s performance or suitability for specific applications. Please conduct necessary tests before use. Thank you for your choice and support!
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