Product Technical Specification

Main Components

Waterborne aliphatic polyurethane resin

Product Features

- Low modulus, high solid content resin for synthetic leather foaming.

- Suitable for dry-process base of waterborne garment leather; soft hand feel and high fullness.

Product Technical Parameters

| Item | Parameter | Unit |
| --- | --- | --- |
| Appearance | Milky white with obvious blue light | — |
| Solid Content | 47±2 | % |
| pH | 6.0~8.0 | — |
| 100% Modulus | 0.5~1.5 | MPa |
| Breaking Strength | ≥5 | MPa |
| Elongation | ≥800 | % |

Precautions

Non-hazardous chemical. Store sealed at 5 ℃~35 ℃, avoid light. Reseal after use. Do not mix with cationic pastes or solvent-based pastes.

The above information only represents our laboratory quality evaluation results and does not guarantee the product’s performance or suitability for specific applications. Please conduct necessary tests before use. Thank you for your choice and support!