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Product Technical Specification
Product Introduction
CN-108 Waterborne Polyurethane Dispersion is an anionic waterborne polyurethane resin using water as the dispersion medium. It features low VOCs, safe, non-toxic, odorless and non-irritating. It offers excellent adhesion to substrates such as PVC and PET, suitable for coatings on PVC, PET and other plastic substrates, as well as for the preparation of water-based inks for PVC, PET and other substrates.

Product Features
1. Eco-friendly emulsion, free of toxic substances including formaldehyde, nonylphenol, heavy metals, polycyclic aromatic hydrocarbons (PAHs) and DMF.
2. Smooth and slippery film formation, high strength, hard and with excellent toughness.
3. Excellent water resistance and outstanding boiling resistance of the coating.
4. Outstanding adhesion to most substrates.

Product Technical Parameters*

	Item
	Parameter
	Unit
	Test Method

	Appearance
	Slightly transparent bluish liquid
	/
	GB/T 14074.1-1993

	Solid Content
	40.00±1.00
	%
	GB/T 2793-1995

	Viscosity
	>10.0
	mPa·s
	GB/T 10247-1998

	pH
	6.5–7.5
	/
	GB/T 14518-1993

	100% Modulus
	12.0–15.0
	MPa
	/

	Tensile Strength
	45.0–50.0
	MPa
	/


*The above parameters are typical results only and shall not be regarded as specifications. Please refer to the actual COA for details.

Storage
1. Store in the original sealed container.
2. Recommended storage temperature: 6–28℃.
3. Use within 6 months from the production date.
4. Avoid direct sunlight and contamination by other substances.

	Prolonged storage at low temperature may cause irreversible damage to the product. Keep the container tightly sealed; otherwise, water evaporation will form an insoluble polymer film on the product surface. Expiry of the 6‑month shelf life does not necessarily mean the product is out of specification. Please test before application to verify its compliance.



Precautions
1. Adding curing agent can improve fastness but may affect the hand feel.
2. Water-based resin added with crosslinking agent must be used within 24 hours.
3. This product is synthesized from special polyester, and the dry film provides excellent water resistance; the water-based emulsion may still have decomposition risk, so advance testing is required for long-term storage and application.









	The above information represents our laboratory quality evaluation results only, and is not a guarantee of the product’s specific performance or suitability for particular applications. Please conduct necessary tests before use. Thank you for your choice and support!
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Hefei Conada New Materials Co. , Ltd.




