Product Technical Specification

Product Introduction

CN-108 Waterborne Polyurethane Dispersion is an anionic waterborne polyurethane resin using water as the dispersion medium. It features low VOCs, safe, non-toxic, odorless and non-irritating. It offers excellent adhesion to substrates such as PVC and PET, suitable for coatings on PVC, PET and other plastic substrates, as well as for the preparation of water-based inks for PVC, PET and other substrates.

Product Features

- Eco-friendly emulsion, free of toxic substances including formaldehyde, nonylphenol, heavy metals, polycyclic aromatic hydrocarbons (PAHs) and DMF.

- Smooth and slippery film formation, high strength, hard and with excellent toughness.

- Excellent water resistance and outstanding boiling resistance of the coating.

- Outstanding adhesion to most substrates.

Product Technical Parameters*

| Item | Parameter | Unit | Test Method |
| --- | --- | --- | --- |
| Appearance | Slightly transparent bluish liquid | / | GB/T 14074.1-1993 |
| Solid Content | 40.00±1.00 | % | GB/T 2793-1995 |
| Viscosity | >10.0 | mPa·s | GB/T 10247-1998 |
| pH | 6.5–7.5 | / | GB/T 14518-1993 |
| 100% Modulus | 12.0–15.0 | MPa | / |
| Tensile Strength | 45.0–50.0 | MPa | / |

*The above parameters are typical results only and shall not be regarded as specifications. Please refer to the actual COA for details.

Storage

- Store in the original sealed container.

- Recommended storage temperature: 6–28℃.

- Use within 6 months from the production date.

- Avoid direct sunlight and contamination by other substances.

Prolonged storage at low temperature may cause irreversible damage to the product. Keep the container tightly sealed; otherwise, water evaporation will form an insoluble polymer film on the product surface. Expiry of the 6-month shelf life does not necessarily mean the product is out of specification. Please test before application to verify its compliance.

Precautions

- Adding curing agent can improve fastness but may affect the hand feel.

- Water-based resin added with crosslinking agent must be used within 24 hours.

- This product is synthesized from special polyester, and the dry film provides excellent water resistance; the water-based emulsion may still have decomposition risk, so advance testing is required for long-term storage and application.

The above information represents our laboratory quality evaluation results only, and is not a guarantee of the product’s specific performance or suitability for particular applications. Please conduct necessary tests before use. Thank you for your choice and support!