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Product Technical Specification
Product Introduction
CN-1080 is an anionic waterborne polyurethane resin using water as the dispersion medium. It features low VOCs, safe, non-toxic, odorless and non-irritating. It provides excellent adhesion to substrates such as PVC, ABS and polyester, and is suitable as an adhesive for plastic substrates including PVC and ABS.

Product Features
1. Eco-friendly emulsion, free of toxic substances such as formaldehyde, nonylphenol, heavy metals, PAHs and DMF.
2. Smooth and firm film, hard with excellent toughness.
3. Excellent water resistance and outstanding cooking resistance of the coating.
4. Outstanding adhesion to most substrates.

Product Technical Parameters*
	Item
	Parameter
	Unit
	Test Method

	Appearance
	Bluish liquid
	—
	GB/T 14074.1-1993

	Solid Content
	40.00±1.00
	%
	GB/T 2793-1995

	Viscosity
	>10.0
	mPa·s
	GB/T 10247-1998

	pH
	6.5–7.5
	—
	GB/T 14518-1993

	100% Modulus
	12.0–15.0
	MPa
	—

	Tensile Strength
	45.0–50.0
	MPa
	—


*The above parameters represent typical results only and shall not be regarded as specifications. Refer to the actual COA for details.

Storage
1. Store in the original sealed container.
2. Recommended storage temperature: 6–28 °C.
3. Use within 6 months from the production date.
4. Avoid direct sunlight and contamination by other substances.

	Prolonged storage at low temperatures may cause irreversible damage to the product. Keep the container sealed; otherwise, water evaporation will form an insoluble polymer film on the surface. Expiration of the 6-month shelf life does not mean the product is out of specification. Test before use to verify compliance with specifications and technical parameters.



Precautions
1. Adding a curing agent can improve fastness but may affect hand feel.
2. Waterborne resin added with crosslinking agent must be used within 24 hours.
3. This product is synthesized with special polyester. The dry film offers excellent water resistance. However, the aqueous emulsion may decompose during long-term storage. Please test in advance before using long-stored product.





	The above information only represents our laboratory quality evaluation results and does not guarantee the product’s performance or suitability for specific applications. Please conduct necessary tests before use. Thank you for your choice and support!
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