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Product Technical Specification
Product Introduction
[bookmark: _GoBack]CN-113 Waterborne Polyurethane Dispersion is a high-performance aromatic waterborne polyurethane resin. It is safe, non-toxic, odorless and non-irritating. The film is transparent, soft with slight tack, smooth in formation and high in gloss. It can be used as a waterborne adhesive for metal, plastic, wood, paper, printing ink, etc., and also as a soft substrate coating for genuine leather, synthetic leather, printing paste, textiles, paper, etc. The environmental protection test results of this product meet the standards of Europe, America and Japan (environmental protection test report can be provided upon request).
Product Features
1. Environmentally friendly emulsion, free of toxic substances such as formaldehyde, nonylphenol, heavy metals, polycyclic aromatic hydrocarbons (PAHs) and DMF.
2. Transparent and soft film with good gloss and excellent flexibility.
3. Excellent water resistance of the coating.
4. Excellent adhesion to most substrates.
5. The hardness of the resin can be adjusted by matching with our company’s CN-115.

Technical Parameters*

	Item
	Parameter
	Unit
	Test Method

	Appearance
	Bluish liquid
	/
	GB/T 14074.1-1993

	Solid Content
	35.00±1.00
	%
	GB/T 2793-1995

	Viscosity
	>30.0
	mPa·s
	GB/T 10247-1998

	pH
	6.0-8.0
	/
	GB/T 14518-1993

	100% Modulus
	3.0-4.0
	MPa
	/

	Tensile Strength
	9.0-10.0
	MPa
	/


*These parameters represent typical results only and shall not be regarded as specifications. Subject to the actual COA.

Storage
1. Store in the original sealed container.
2. Recommended storage temperature: 6-28℃.
3. Use within 6 months from the production date.
4. Avoid direct sunlight and contamination by other substances.

	Prolonged storage at low temperature will cause irreversible damage to the product. Keep the container sealed; otherwise, water evaporation will form an insoluble polymer film on the product surface. Expiry of the above 6-month period does not mean the product is out of specifications or technical parameters. Please test before use to confirm compliance with specifications or technical parameters.



Precautions
1. Adding curing agent can improve fastness but may affect hand feel.
2. Waterborne resin added with crosslinking agent must be used within 24 hours.
3. This product is synthesized with special polyester, and the dry film has excellent water resistance; the waterborne emulsion may decompose during long-term storage, so please test in advance before use.










	The above information only represents our quality evaluation results obtained from our laboratory and is not a guarantee that the product has certain properties or meets specific applications. Please conduct specific tests as required before use. Thank you for your choice and support!
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Hefei Conada New Materials Co. , Ltd.




