Product Technical Specification

Product Introduction

CN-116 is a high-performance aliphatic waterborne polyurethane resin. It is safe, non-toxic, odorless and non-irritating. The film is transparent, continuous, smooth, with high hardness and good gloss. It is a one-component waterborne coating for woodware, rattan ware, bamboo ware, metal, paper, plastic, glass and other substrates.

Product Features

- co-friendly emulsion, free of toxic substances such as formaldehyde, nonylphenol, heavy metals, polycyclic aromatic hydrocarbons (PAHs) and DMF.

- Transparent, smooth film with good gloss.

- Excellent water resistance and weather resistance of the coating.

- High hardness, up to 1–2H.

Technical Parameters*

| Item | Parameter | Unit | Test Method |
| --- | --- | --- | --- |
| Appearance | Bluish liquid | / | GB/T 14074.1-1993 |
| Solid Content | 35.00±1.00 | % | GB/T 2793-1995 |
| Viscosity | >30.0 | mPa·s | GB/T 10247-1998 |
| pH | 6.0–8.0 | / | GB/T 14518-1993 |
| 100% Modulus | 16.0–18.0 | MPa | / |
| Tensile Strength | 47.0–55.0 | MPa | / |

*These parameters represent typical results only and shall not be deemed as specifications. Subject to the actual Certificate of Analysis (COA).

Storage

- Store in the original sealed container.

- Recommended storage temperature: 6–28 °C.

- Use within 6 months from the production date.

- Avoid direct sunlight and contamination by other substances.

Prolonged storage at low temperature will cause irreversible damage to the product. Keep the container sealed; otherwise, water evaporation will form an insoluble polymer film on the surface. Expiry of the 6-month shelf life does not mean the product is out of specification. Please test before use to verify its compliance.

Precautions

- Adding a curing agent can improve fastness but may affect the hand feel.

- Waterborne resin with crosslinking agent must be used within 24 hours.

- This product is synthesized with special polyester; the dry film provides excellent water resistance. The waterborne emulsion may degrade during long-term storage, so pre-testing is recommended before use.

The above information reflects our internal quality evaluation results from laboratory testing. It is not a guarantee of product performance or suitability for specific applications. Please conduct necessary tests before application. Thank you for your choice and support!