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Product Technical Specification
Product Introduction
CN-6017 is an anionic waterborne polyurethane resin. It is safe and eco-friendly, with transparent film, smooth film formation, medium-hard non-tacky surface, and good temperature resistance and aging resistance. It can be used as a waterborne adhesive or coating for plastics (PVC, PC, ABS, etc.), paper, leather, etc.

Product Features
1. Transparent film, smooth film formation, medium-hard non-tacky surface, and excellent flexibility.
2. Excellent water resistance and anti-blocking property of the coating.
3. Can be used with our company’s series of waterborne curing agents (CN-G118/120) to enhance resin performance.

Product Technical Parameters*
	Item
	Parameter
	Unit
	Test Method

	Appearance
	Bluish liquid
	—
	GB/T 14074.1-1993

	Solid Content
	36.00±1.00
	%
	GB/T 2793-1995

	Viscosity (25℃)
	100–4000
	mPa·s
	GB/T 10247-1998

	pH
	6.5–7.5
	—
	GB/T 14518-1993

	100% Modulus
	3.0–5.0
	MPa
	—

	Tensile Strength
	28.0–30.0
	MPa
	—

	Elongation at Break
	200–280
	%
	—


*The above parameters represent typical results only and shall not be regarded as specifications. Refer to the actual COA for details.

Storage
1. Store in the original sealed container.
2. Recommended storage temperature: 6–28 °C.
3. Use within 6 months from the production date.
4. Avoid direct sunlight and contamination by other substances.

	Prolonged storage at low temperatures may cause irreversible damage to the product. Keep the container sealed; otherwise, water evaporation will form an insoluble polymer film on the surface. Expiration of the 6-month shelf life does not mean the product is out of specification. Test before use to verify compliance with specifications and technical parameters.



Precautions
1. Adding a curing agent can improve fastness but may affect hand feel.
2. Waterborne resin added with crosslinking agent must be used within 24 hours.
3. This product is an anionic resin. Do not mix with other cationic resins or additives. Our polyurethane thickener can be used to adjust emulsion viscosity.
4. This product is synthesized with special materials. The dry film offers excellent water resistance. However, the aqueous emulsion may decompose during long-term storage. Please test in advance before using long-stored product.




	The above information only represents our laboratory quality evaluation results and does not guarantee the product’s performance or suitability for specific applications. Please conduct necessary tests before use. Thank you for your choice and support!
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Hefei Conada New Materials Co. , Ltd.




