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Waterborne Polyurethane Dispersion


Product Technical Specification
Product Introduction 
CN-806 is a high-solid aromatic waterborne polyurethane dispersion independently developed by our company, with excellent performance reaching the advanced domestic level. This product is safe, non-toxic, odorless and non-irritating, and can be used as a coating for flexible substrates such as plastics and textiles (especially nylon fabrics). Its environmental test results meet the standards of Europe, the United States and Japan (environmental test reports can be provided upon request).

Product Features
1. Eco-friendly emulsion, free of toxic substances such as formaldehyde, nonylphenol, heavy metals, PAHs and DMF.
2. Excellent toughness of the formed film.
3. Good elongation and low-temperature flexibility.
4. Particularly outstanding adhesion to nylon fabrics. 

Product Technical Parameters*
	Item
	Parameter
	Unit
	Test Method

	Appearance
	Milky white with strong blue tint
	—
	GB/T 14074.1-1993

	Solid Content
	36.00±1.00
	%
	GB/T 2793-1995

	Viscosity (25℃, Rotor 3#, 60rpm)
	＞100
	mPa·s
	GB/T 10247-1998

	pH
	6.5–7.0
	—
	GB/T 14518-1993

	Ionic Type
	Anionic
	—
	—


*The above parameters represent typical results only and shall not be regarded as specifications. Refer to the actual COA for details.

Application Scope
Can be used as a coating for flexible substrates such as plastics and textiles (especially nylon fabrics).

[bookmark: _GoBack]Packaging , Transportation , Storage
1. Packaging: Plastic drums, 50 kg and 125 kg.
2. Transportation: Shipping or self-pickup.
3. Storage:① Store in a ventilated and dry place at 5℃–35℃, avoid direct sunlight or freezing. Shelf life: 6 months.② Non-dangerous goods.

	Prolonged storage at low temperatures may cause irreversible damage to the product. Keep the container sealed; otherwise, water evaporation will form an insoluble polymer film on the surface. Expiration of the 6-month shelf life does not mean the product is out of specification. Test before use to verify compliance with specifications and technical parameters.



Precautions
1. Adding a curing agent can improve fastness but may affect hand feel.
2. The slurry with crosslinking agent must be used up within 24 hours.
3. Since the product is synthesized from special hydrolysis-resistant polyester, the dry film has good hydrolysis resistance. However, slow hydrolysis may still occur during storage of the dispersion. It is recommended to use the product immediately after purchase.



	The above information only represents our laboratory quality evaluation results and does not guarantee the product’s performance or suitability for specific applications. Please conduct necessary tests before use. Thank you for your choice and support!



— 1 —

image1.png




image2.png
SEREMNEFHAEBRARE

Hefei Conada New Materials Co. , Ltd.




